Heterogeneous Rhenium Catalysts supported on Ceria for Deoxydehydration of Polyols with Hydrogen

Keiichi Tomishige*, Yoshinao Nakagawa, Masazumi Tamura

Department of Applied Chemistry, School of Engineering, Tohoku University, 6-6-07, Aoba, Aramaki, Aoba-ku, Sendai, Miyagi 980-8579, Japan

*Email: tomi@erec.che.tohoku.ac.jp

Chemical composition of the feedstock from biomass and biomass-based building blocks has much higher oxygen contents than that from crude oil. It has been known that the target products such as monomers for the polymer synthesis have comparatively lower oxygen content, and the reaction to decrease the oxygen content is important. It has been known that C3-C6 sugar alcohols (glycerol, erythritol, xylitol, and sorbitol) are regarded as promising building blocks in the biomass refinery, on the other hand, these compounds are over-functionalized. Therefore, the selective conversion is necessary to obtain appropriately functionalized compounds. A method is the selective C-O hydrogenolysis which demands the recognition of the target C-O bond among various kinds of C-O bonds. This enables the production of valuable chemicals such as diols, mono-ols, alkanes in high yield. ReOx-modified Ir metal catalyst (Ir-ReOx) is reported to be effective to the selective hydrogenolysis of polyols and cyclic ethers in water solvent as shown in Figure 1 [1]. The hydrogenolysis of tetrahydrofurfuryl alcohol to 1,5-pentanediol proceeds over Ir-ReOx/SiO2 with high selectivity (Figure 1, [1]). In addition, the combination of Ir-ReOx/SiO2 with H-ZSM-5 gives n-alkanes and hexanols from cellulose, sugars, and sugar alcohols in high yield with the deep C-O hydrogenolysis and without C-C bond dissociation and skeletal isomerization (Figure 1, [1]). Ir-ReOx/SiO2 catalyzes the hydrogenolysis of glycerol to 1,3-propanediol with high selectivity (Figure 1 [1]). However, this Ir-ReOx/SiO2 was applied to the hydrogenolysis of erythritol, and the synthesis of the specific diol is much more difficult, and various kinds of products were co-produced [1]. The deoxydehydration is utilized for the selective conversion and we have developed the heterogeneous catalysts for the deoxydehydration reaction. Recently we found that ReOx-Pd/CeO2 showed excellent performance for simultaneous hydrodeoxygenation of vicinal OH groups in various substrates via deoxydehydration. High yield (>99%), turnover frequency, and turnover number were obtained in the reaction of 1,4-anhydroerythritol to tetrahydrofuran [2, 3]. This catalyst is also applicable to the conversion of sugar alcohols, and mono-alcohols and diols were obtained in high yields from substrates with even and odd numbers of OH groups, respectively [2]. In addition, ReOx-Au/CeO2 catalyzed the conversion of glycerol and erythritol to allyl alcohol and 1,3-butadiene in high yield (91% and 81%), respectively [4].

Keywords: biomass; sugar alcohol; cyclic ether; hydrogenolysis; hydrodeoxygenation; deoxydehydration.

Reference

[1] Tomishige, K.; Tamura, M.; Nakagawa, Y. Chem. Rec. 2014, 14, 1041-1054.

[2] Ota, N.; Tamura, M.; Nakagawa, K.; Okumura, K.; Tomishige, K. Angew. Chem. Int. Ed. 2015, 54, 1897-1900.

[3] Ota, N.; Tamura, M.; Nakagawa, K.; Okumura, K.; Tomishige, K. ACS Catal. 2016, 6, 3213-3226.

[4] Tazawa, S.; Ota, N.; Tamura, M.; Nakagawa, K.; Okumura, K.; Tomishige, K. ACS Catal. 2016, 6, 6393-6397

Keiichi Tomishige received his B.S., M.S. and Ph.D. from Graduate School of Science, Department of Chemistry, The University of Tokyo with Prof. Y. Iwasawa. During his Ph.D. course in 1994, he moved to Graduate School of Engineering, The University of Tokyo as a research associate and worked with Prof. K. Fujimoto. In 1998, he became a lecturer, and then he moved to Institute of Materials Science, University of Tsukuba as a lecturer in 2001. Since 2004 he has been an associate professor, Graduate School of Pure and Applied Sciences, University of Tsukuba. Since 2010, he is a professor, School of Engineering, Tohoku University. His research interests are the development of heterogeneous catalysts for 1) production of biomass-derived chemicals, 2) direct synthesis of organic carbonates from CO2 and alcohols, 3) steam reforming of biomass tar, and 4) syngas production by natural gas reforming.

He is Associate Editor of Fuel Processing Technology (2014/2-), Editorial board of Applied Catalysis A (2009/4-), Editorial advisory board of ACS Catalysis (2013/11-), International Advisory Board of ChemSusChem (2015/1-) and Advisory Board of Green Chemistry (2016/8-).